DESIGN AND DEVELOPMENT OF LIGNIN BASED UV PROTECTANTS FOR SKINCARE APPLICATION

A PROJECT REPORT

Submitted by

| JANANI.M | (962620214016) |
| --- | --- |
| MADHAVAN.G | (962620214028) |
| MIDHUNA.TM | (962620214030) |
| SANMUGANATHAN.P | (962620214048) |

In partial fulfillment for the award of the degree

of

BACHELOR OF TECHNOLOGY

in
BIOTECHNOLOGY

UDAYA SCHOOL OF ENGINEERING, VELLAMODI

ANNA UNIVERSITY: CHENNAI 600 025

MAY 2024

ANNA UNIVERSITY: CHENNAI 600 025

BONAFIDE CERTIFICATE

Certified that this project Report “DESIGN AND DEVELOPMENT OF LIGNIN BASED UV PROTECTANTS FOR SKINCARE APPLICATION” is the bonafide work of JANANI.M, MADHAVAN.G, MIDHUNA.TM, SANMUGANATHAN.P who carried out the work under my supervision.

| SIGNATURE Dr.L.R.MONISHA MIRIAM, M.Tech.,Ph.D. HEAD OF THE DEPARTMENT, Department of Biotechnology, Udaya School of Engineering, Udaya Nagar, Vellamodi, Kanyakumari District, Tamil Nadu, India. | SIGNATURE Dr.D.DEVINA MERIN, M.Tech.,Ph.D. SUPERVISOR Department of Biotechnology, Udaya School of Engineering, Udaya Nagar, Vellamodi, Kanyakumari District Tamil Nadu, India. |
| --- | --- |

Submitted for the B.Tech Degree University Examination held on......................

Internal Examiner                                                 External Examiner

ACKNOWLEDGEMENT

First of all I would like to thank the almighty God for giving me the strength and health to complete this project successfully.

At the outset, I would like to express my sincere gratitude to our beloved chairman Er. C. THAYAPARAN M.E., who has always encouraged in the academic activities.

I express my sincere thanks and gratitude to the dynamic Principal                  Dr. S. JOTHIBASU M.E., MBA., Ph.D for providing all the facilities indispensable during the course of my project.

I would like to express my deep sense of gratitude to                                  Dr. L. R. MONISHA MIRIAM., M.Tech., Ph.D, Head of the Department, Department of Biotechnology, Udaya school of Engineering, Vellamodi, for his moral support and valuable suggestion during my project work.

I extend the sincere thanks to my Internal  Guide                                        Dr. D. DEVINA MERIN., M.Tech., Ph.D, Superviser, Department of Biotechnology, Udaya school of Engineering, Vellamodi, for her guidance and support.

Finally, I take this opportunity to extend my deep appreciation to my beloved parents and friends, for all that they meant to us during the crucial times of the completion of this project work.

ABSTRACT

Lignin has been suggested as a promising candidate for cosmetic application due to its remarkable potential to absorb ultraviolet rays and distinctive antioxidant activity. This study to produce lignin-based sunscreen using an assisted enhancer with NaOH. Lignin is a natural UV-blocking material. Lignin-based sunscreen is to find that the sunscreen performance improves with UV radiation time. Coconut husks are similar to other lignocellulosic biomass, primarily composed of cellulose, hemicelluloses and lignin. On a dry-weight basis, coconut husk contains 41% of lignin. One such resource is coconut husk, a material usually discarded during the copra extraction process coconut husk has higher lignin content than other woody biomass. due to its high lignin content coconut husk has been recognized as having a variety of applications. Despite its significant UV blocking potential the intrinsic dark color of lignin results in the unavoidable dark color of lignin-based sunscreens which significantly limits its wide application. Future perspectives of lignin-inspired sunscreen production were discussed to suggest promising approaches for facile and green manufacturing of natural sunscreen from lignin extraction.

Key words: Lignin, Coconut husk, Sunscreen, UV rays, Skincare, Shea butter

| TABLE OF CONTENTS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| CHAPTER NO | TITLE |  |  |  |  | PAGE NO |
|  | ABSTRACT |  |  |  |  | IV |
|  | LIST OF TABLES |  |  |  |  | VIII |
|  | TABLE OF FIGURES |  |  |  |  | IX |
|  | LIST OF SYMBOLS AND ABBREVIATIONS |  |  |  |  | X |
| I | INTRODUCTION |  |  |  |  | 1 |
|  | 1.1 |  | AIM & OBJECTIVES |  |  | 6 |
|  | 1.2 |  | WORK PLAN |  |  | 7 |
| II | REVIEW OF LITERATURE |  |  |  |  | 8 |
|  | 2.1 |  | LIGNIN |  |  | 8 |
|  | 2.2 |  | TYPES OF LIGNIN |  |  | 9 |
|  | 2.3 |  | VARIETIES OF SOURCES |  |  | 11 |
|  | 2.4 |  | USES OF LIGNIN |  |  | 13 |
|  | 2.5 |  | LIGNIN FROM COCONUT |  |  | 15 |
|  | 2.6 |  | EXTRACTION OF LIGNIN FROM COCONUT HUSK OR COIR |  |  | 17 |
| III | MATERIALS AND METHODS |  |  |  |  | 18 |
|  | 3.1 | MATERIALS |  |  |  | 18 |
|  | 3.2 | EXTRACTION OF LIGNIN |  |  |  | 18 |
|  |  | 3.2.1 |  |  | Acid alkali method | 18 |
|  |  | 3.2.2 |  |  | Microwave assisted extraction | 18 |
|  | 3.3 | OPTIMIZATION USING OVAT |  |  |  | 19 |
|  | 3.4 | CHARACTERIZATION |  |  |  | 19 |
|  |  | 3.4.1 |  |  | FTIR | 19 |
|  | 3.5 | PREPARATION OF SUNSCREEN LOTION |  |  |  | 20 |
|  |  | 3.5.1 |  |  | Phase I | 20 |
|  |  | 3.5.2 |  |  | Phase II | 20 |
|  | 3.6 | IN VITRO SPF ASSAY OF CREAM |  |  |  | 21 |
|  | 3.7 | EVALUATION OF CREAM |  |  |  | 22 |
|  |  | 3.7.1 |  | Ph of the Cream |  | 22 |
|  |  | 3.7.2 |  | Dye test |  | 22 |
|  |  | 3.7.3 |  | Homogeneity |  | 23 |
|  |  | 3.7.4 |  | Appearance |  | 23 |
|  |  | 3.7.5 |  | After feel |  | 23 |
|  |  | 3.7.6 |  | Type of smear |  | 23 |
|  |  | 3.7.7 |  | Removal |  | 23 |
|  |  | 3.7.8 |  | Irritancy test |  | 23 |
|  |  | 3.7.9 |  | Acid value |  | 24 |
|  |  | 3.7.10 |  | Saponification value |  | 24 |
| IV | RESULTS AND DISCUSSION |  |  |  |  | 25 |
|  | 4.1 | LIGNIN YIELD, RECOVERY AND PURITY |  |  |  | 25 |
|  | 4.2 | EFFECT OF PROCESS VARIABLES IN EXTRACTION OF LIGNIN (OVAT) |  |  |  | 26 |
|  |  | 4.2.1 |  | Effect of microwave power |  | 26 |
|  |  | 4.2.2 |  | Effect of alkali concentration |  | 26 |
|  |  | 4.2.3 |  | Effect of liquid and solid ratio |  | 26 |
|  | 4.3 | FT-IR LIGNIN: |  |  |  | 28 |
|  | 4.4 | INVITRO SPF ASSAY OF CREAM |  |  |  | 29 |
|  | 4.5 | SELECTION OF OPTIMIZED FORMULATION |  |  |  | 30 |
|  | 4.6 | PHYSIOCHEMICAL STUDIES |  |  |  | 30 |
|  | 4.7 | STABILITY |  |  |  | 32 |
| V | CONCLUSIONS |  |  |  |  | 34 |
|  | REFERENCES |  |  |  |  | 35 |

LIST OF TABLES

| TABLE NO | Name of the Table | PAGE NO. |
| --- | --- | --- |
| 4.1 | Yields and recoveries achieved in the procedures. | 21 |
| 4.2 | SPF of the formulated and marketed sunscreen: | 24 |
| 4.3 | SPF of the formulated and marketed sunscreen: | 27 |
| 4.4 | Stability evaluation by physicochemical parameters (F6) | 35 |
| 4.5 | Stability evaluation by physicochemical parameters (F10) | 38 |

LIST OF FIGURES

| FIGURE NO | NAME OF THE FIGURES | PAGE NO |
| --- | --- | --- |
| 4.2.1 | Effect on Microwave power | 27 |
| 4.2.2 | Effect of Alkali | 28 |
| 4.2.3 | Effect Of Solid liquid Ration | 29 |

LIST OF ABBREVIATIONS

| % | Percentage |
| --- | --- |
| cm | Centimeter |
| g | Gram |
| Hrs | Hours |
| M | Molar |
| mgl | Milligrams per liter |
| Min | Minute |
| ml | Millilitre |
| ml | Mililitre |
| nM | Milli molor |
| nm | Nano meter |
| oC | Degree celsius |
| pH | -log(H) |
| ppm | Parts per million |
| rpm | Rotation per minute |
| rpm | Revolution per minute |
| S | Second |
| T | Temperature |
| UV | Ultraviloet |
| μg | Milligram |
| μl | Micro litre |

chAPTER I

INTRODUCTION

Lignin is one of the most promising renewable resource options. Furthermore, lignin is also the second most abundant biopolymer in lignocellulosic biomass after cellulose. Lignin is a major source of aromatic compounds in nature(Wang, Pu et al. 2019). It has recently attracted much attention as a potential ultraviolet (UV) blocking material due to its availability of functional chromophore groups that act as UV absorbers, including conjugated phenol quinoid structures, ketones, and intramolecular hydrogenbonds(Wypych 2020).  lignin is also a good natural antibacterial and antioxidant agent. As a result of these distinguishing characteristics, lignin in sunscreens is gaining popularity(Ariyanta, Santoso et al. 2023). Because of its low cytotoxicity, lignin can create ecologically friendly and safe functional lignin-based products, such as sunscreens.(Ariyanta, Santoso et al. 2023).In recent years, attention has focused on lignin as a safer and biodegradable substitute for synthetic UV absorbers in sunscreens. Found in trees and other lignocellulosic plants, native lignin is a polyphenolic polymer that acts as the glue between cellulosic woody cells(Widsten 2020). During kraft (sulfate), soda, organosolv and other chemical pulping processes of lignocellulosic raw materials, lignin undergoes partial depolymerization and other structural changes and is dissolved in the black liquor or organic solvent(Gavrilescu 2020). Unless burnt at the pulp mill for energy, this mostly water-insoluble by-product (technical lignin) can be recovered for various value-added applications(Margarida Martins, Carvalheiro et al. 2024). Lignocellulosic biorefineries and agricultural by-products are becoming another important source of technical lignins(Widsten 2020).

UV-B has a longer wavelength that ranges from 290 nm to 320 nm, and, as a result, is not only able to penetrate the ozone layer but also penetrates the epidermis layer of the skin and becomes a triggering factor for sunburn(Sen Mandi and Sen Mandi 2016). UV-B usually appears around 11 am until 1 pm. UV-A has a wavelength of 320 nm to 400 nm and consequently penetrates the layers of the epidermis, dermis, and sub-skin tissue and is considered a triggering factor for skin cancer. UV-A appears throughout the day, even from morning to evening(Sari, Rois et al. 2022). When UV radiation penetrates the skin, its primary target is oxygen molecules beneath the epidermis. This results in the formation of various free radical compounds, including reactive oxygen species (ROS), hydroxyl radicals, lipid alkyl radicals, and so on(Ganguly, Hota et al. 2021). The presence of these free radicals in the skin can cause various forms of skin damage, such as skin aging, darkening of pigments, and even skin cancer(Emerit 1992). lignin is widely studied as an active ingredient in sunscreens to increase the sun protection factor (SPF) value contained in sunscreens.(Sari, Rois et al. 2022).

Coconut husk (cocos nucifera ) the fibrous external portion of the fruit of coconut palms, is a by-product of the copra extraction process and is generally considered as a waste(Mat, Abdul Kari et al. 2022). A variety of uses have been proposed for coconut husk lignin, which is present at levels of up to 33% by weight of the husk." The applications range from the fabrication of particle board agglomerated by "its own resin" l2 to the hydrogen chloride extraction of lignin to be used as an additive in the formulation of reinforced plastics(Salunkhe and Kadam 1995)." One important aspect that, in our view, has been omitted in these efforts is the knowledge of the approximate structure and characteristics of the lignin involved(Vanholme, Demedts et al. 2010). Also overlooked have been the general extractability features of the polymer, which are of the utmost importance since its physicochemical properties depend highly on the method of isolation used(Domínguez-Rodríguez, Marina et al. 2017)Since chemical reactivity and potential applications of the material are intimately connected to these properties, it would be desirable to know them in order to devise further studies in this area(Váquez‐Torres, Canché‐Escamilla et al. 1992).

Cocos nucifera L. species is a plant native to tropical countries and belongs to the Arecaceae family, with a very high economical value(Yang, Iqbal et al. 2018). In Brazil, it is widely distributed on the Northeastern coast and North of Brazil, where different varieties are found, among them, a dwarf one, composed of yellow, green and red cultivars. Coconut husk fiber is a byproduct of Cocos nucifera processing(Vieira, Santana et al. 2024). Its accumulation as waste can cause serious environmental and social problems. At recent years, special attention has been paid to minimizing the environmental negative impacts of these fibers. Several patents reported the application of coconut husk fiber, in the production of agricultural substrates, in the automotive industry, in civil construction and in landscaping, among other technologies(Gomes da Silva, Gouveia et al. 2020). Its uses as adsorbents of organic substances and toxic pollutants had been, also described. In addition, its fibers are also widely used in traditional medicine in several countries(Karić, Maia et al. 2022).

The use of sunscreens is a more effective alternative against the harmful effects caused by UV rays(Gasparro 2000). These products, initially developed and intended to protect the skin against sunburn, have expanded their action in protection against other harmful effects such as premature aging, unwanted pigmentation and loss of collagen(Ngoc, Tran et al. 2019). In this sense, several publications have demonstrated the use of phenolic-rich plant extracts, as active ingredients in protective formulations. In addition to the photoprotective action, these extracts have antioxidant and antiglycation properties that can reduce the effects of oxidative damage, caused by the UV radiation, besides offering stability to sunscreens and assisting in the preservation of collagen. In previous studies, the presence of flavonoids such as quercetin and catechin in the ethanolic extract of coconut husk fiber of the yellow dwarf variety was reported. These flavonoids have photoprotective action, so the use of this extract in formulations is worth evaluating(Oliveira, Valentim et al. 2021).

Lignin is a natural UV-blocking material; it exhibits excellent UV absorption ability owing to its aromatic structure and the presence of numerous phenolic, ketone, and intramolecular hydrogen bonds(Tran, Phan et al. 2021). Recently, the utilization of lignin as a replacement for conventional mineral and synthetic UV protection ingredients in sunscreens has been recognized as an attractive and promising concept from the viewpoint of renewable and sustainable manufacturing of lignin-based products(Ariyanta, Santoso et al. 2023). Despite its significant UV-blocking potential, the intrinsic dark color of lignin results in the unavoidable dark color of lignin-based sunscreens, which significantly limits its wide applicatio(Kim, Park et al. 2023). Therefore, the present review focuses on providing a comprehensive insight into lignin-based sunscreens. The positive effects of the sunblocking ability of lignin and the drawbacks associated with lignin-based sunscreens, from the viewpoint of cosmetic appearance, were investigated in detail(Henriksson and Nordell 2023). To address the bottlenecks of lignin-based sunscreens, several methods, including fractionation and modification on the chemical structure, morphology, and particle size of lignin, were subsequently developed(Espinoza-Acosta and Figueroa-Espinoza 2022). In addition, future perspectives of lignin-inspired sunscreen production were discussed to suggest promising approaches for a facile and green manufacturing of natural sunscreens from lignin(Piccinino 2019)

1.1  AIM &OBJECTIVES

To design and development of lignin based UV protectants or sunscreen for skin care application.

- Selection of efficient methodology for lignin extraction from coconut husk waste

- Development of Lignin based UV protectant for skin care applications

- It has good ultraviolet (UV) absorption and antioxidant properties.

- Protection against oxidative stress

1.2  WORK PLAN

Collection of plant

Sun dried

Drying

Milling

Physiochemical  method

Conventional method

Extraction

Microwave assisted extraction

Acid alkali method

Characterization

Formulation

CHAPTER II

REVIEW OF LITERATURE

2.1 LIGNIN:

Lignin is the most abundant natural phenolic polymers in the world. In nature, lignin polymer usually forms ether or ester linkages with hemicellulose which is also associated with cellulose. Therefore, these nature polymers construct a complicated and valuable lignocellulose polymer(Upton and Kasko 2016). Different sources of lignocellulose contain different ratios of these constructive polymers. In hardwood stem, the xylem usually contains 40–55% of cellulose, 24–40% of  hemicellulose and 18–25% of lignin, while the softwood stem contains 45–50% of cellulose, 25–35% of  hemicellulose and 25–35% of lignin(Chio, Sain et al. 2019)

Depending on the usedprocess for isolating the technical lignin its chemical properties such as composition, molecular weight, molecular structure may be impaired generating different types of lignin, with different types of applications in biorefinery platform (Erdocia, Hernández-Ramos et al. 2021). They also differ in physical properties such as solubility, hydrophobicity and hydrophilicity of lignin. Because of these differences, each technical lignin must be considered individually. The pulp mill is the main commercial source of lignin(Souza, Gomes et al. 2020).

In the kraft (and soda) pulping process, on the other hand, the lignin is only water soluble in alkaline solution. Increased water solubility can, however, be achieved through introduction of sulfonate groups via the sulfomethylation reaction (Konduri and Fatehi 2015). At present, such lignins are commercially available, although the production is rather small, with uses such as dispersant for dye pigments. Despite several decades of research about the possibilities of utilizing kraft and soda lignins in material systems such as carbon fibers, polyurethanes, phenol-formaldehyde plastics, adhesives, and others no commercially viable technology has yet been developed within these areas (Gellerstedt 2015).

Organosolv lignin contains little ash relative to other types of industrial lignin (e.g. that obtained with the kraft process), which facilitates its combustion. In this work, the Organosolv process was used to delignify lignocellulosic material from wheat straw and quantified residual lignin in the black liquor with a view to its use for energy production. The starting material was delignified with ethanol–water and acetone–water mixtures in the presence of various acids; this facilitated recycling of the solvent and recovery of dissolved lignin(de la Torre, Moral et al. 2013).

Organosolv processes, on the other hand, especially those that do not use catalysts, generate a large amount of a high-quality lignin which is relatively pure, primarily unaltered and less condensed than other pre-treatment lignins. These ‘‘unaltered” lignins are expected to play an important role in the near future as raw materials for the production of bio-products because they are soluble in many organic solvents and could find applications in the fields of adhesives, fibres, films and biodegradable polymers. A number of processes involving organic solvents that allow both conventional and alternative raw materials to be efficiently delignified have been reported(Quesada-Medina, López-Cremades et al. 2010).

2.2 TYPES OF LIGNIN

Softwood kraft lignin can be expected to be more uniform between wood species due to structural similarity with the lignin containing only one predominant 15type of monolignol as building block (guaiacyl-propane units). This makes it important to obtain an understanding of structural features, reactivity and thermal properties for this type of lignin in order to assist in the development of large scale kraft lignin-based products. In this review, the comprehensive but scattered structural information on softwood kraft lignin that is available in the literature has therefore been summarized and critically evaluated(Gellerstedt 2015).

Hardwood lignin is made of coniferyl alcohol and sinapyl alcohol, forming the macromolecules guaiacyl (G) and syringyl (S), respectively. Softwood lignin contains only guaiacyl units in which one of the ortho-positions next to the phenol is free and hence more easily branched and/or crosslinked. In contrast, hardwood lignin that contains both guaiacyl and syringyl units, has a more linear structure compared to softwood. Softwoods lignin appears to vary little amongst species], whereas hardwood lignins vary greatly between species with a wide range of syringyl-to-guaiacyl ratio (S/G ratio) within its structure. the hardwood kraft lignin properties depend upon the feedstock from which they are obtained (wood species), the extraction method employed, and downstream purification processes. The depolymerization of hardwood lignin generally results in high aromatic monomer yields because these feedstocks typically contain high S/G)ratios(Jardim, Hart et al. 2020).

Grass lignin is a complex hydrophobic hetero-phenolic polymer primarily composed of three phenolic alcohols: p-coumaryl alcohol (H), coniferyl alcohol (G), and sinapyl alcohol (S); two hydroxycinnamic acids: p-coumaric acid (pCA)and ferulic acid (FA); four hydroxycinnamate-phenolic conjugates: γ-p-coumaroylated coniferyl alcohol (pCA-G) and γ-p-coumaroylatedsinapyl alcohol (pCA-S), feruloylated coniferyl alcohol (G-FA), and feruloyl sinapyl alcohol (S-FA); and thus far one known flavone: tricin, and many additional conjugated derivatives found in lower concentrations. Grass lignin monomers are synthesized in the phenylpropanoid and flavone pathways, pass through the cell membrane, and are polymerized in secondary cell walls.The purpose of this review is threefold: to present the current models of grass lignin synthesis, translocation, and polymerization; to highlight how lignin contributes to grass stress resistance; and to suggest future avenues of research that may benefit both cereal breeders and valorization engineers(Peracchi, Panahabadi et al. 2024).

2.3 VARIETIES OF SOURCES

Sugarcane is a large perennial tropical grass belonging to the family Gramineae and the genus Saccharum. Sugarcane is a major crop cultivated globally for sugar production. Its distinguishing features are high biomass yield, sucrose content, and efficiency in accumulating solar energy. After the harvest of sugarcane, leaves and tops are left in the field while the sugarcane stalks are transported to sugar mills for the extraction of cane juice for sugar production.  Two major by-products from the sugarcane industry are the harvest residue (straw) and the fibrous fraction following juice extraction (bagasse). These post-harvest by-products have been suggested as an abundant and inexpensive source of lignocellulosic biomass. Sugarcane bagasse (SCB) and sugarcane straw (SCS) are composed of cellulose, hemicellulose, and lignin, with lower amounts of extractives and ash. In the specific case of sugarcane lignin, it is greatly acylated (p-coumaroylation) at their side chains, contains tricin flavonoid units, and hasferulate residues cross-coupled between arabinoxylan and lignin. Studies have shown that SCB and SCS lignins are structurally different, the first one is syringyl-rich with predominance of alkyl-aryl ether substructures, whereas SCS is a guaiacyl-rich lignin with higher amounts of condensed structures(Antunes, Mota et al. 2022).

Agricultural fiber sources such as wheat straw, wheat bran, and oat hull are abundant resources of lignin, cellulose, and hemicelluloses. Although these fiber sources have a relatively lower value compared to wood and other plant fibers, their annual output is considerable. Wheat straw, for example, it is an abundant byproduct from wheat production. It is an annually renewable fiber resource that is available in large quantities in many regions of the world. Nearly 733 million tons hectares of wheat are estimated to be cultivated annually worldwide. The use of wheat straw could open new markets for these agricultural crop residues and improve the rural agriculture-based economy(Zhang, Larsson et al. 2022).

Wood, used by human societies for millennia, remains one of the world’s most abundant raw materials for industrial products and renewable energy. Wood is the secondary xylem of vascular plants, a tissue formed from the terminal differentiation of the inner side of the cambial meristem for vertical and horizontal transport of water, nutrients, and extractives. The secondary cell wall structure and composition of wood are the primary determinants of its physical and chemical properties, and of its energy content. Wood is typically composed of about 25% lignin, and 70% cellulosic carbohydrates, with roughly 45% cellulose and 25% hemicelluloses  (Novaes, Kirst et al. 2010).

Woods showed more lignin derivatives than lipid and carbohydrate

derivatives, with a higher variety of compounds detected and abundance of them. The toasting led to an increase in the concentrations of most of these compounds, and this increase is especially important in acacia, chestnut and ash woods. The cis and trans Extracts of wood from acacia, European ash, American ash, chestnut, cherry, and three oak species (Quercus pyrenaica, Quercus alba and Quercus petraea) before and after toasting in cooperage were studied by GC−MS. 110 compounds were detected, and 97 of them were isomers of β-methyl-γ-octalactone and isobutyrovanillone were only detected in oak wood, 3,4-dimethoxyphenol and 2,4-dihydroxybenzaldehyde only in acacia wood, and p-anisaldehyde and benzylsalicylate only in cherry wood, before and after toasting, and these compounds could be considered chemical markers for each one of these woods(Fernandez de Simon, Esteruelas et al. 2009).

2.4 USES OF LIGNIN

98% of lignin produced in the papermaking and pulping industry is used for combustion heating or power generation. Less than 2% of lignin is used in more valuable fields, mainly in the formulation of dispersants, adhesives, and surfactants. Asphalt is one of the most important materials in pavement engineering. It is a dark brown complex mixture composed of hydrocarbons with different molecular weights and their non-metallic derivatives. Because the chemical structure of lignin is similar to that of asphalt, it is a carbon-based hydrocarbon material. More researchers studied the application of lignin in pavement engineering. In this paper, the structure, application, and extraction technology of lignin  were summarized. This is a review article describing the different applications of lignin in pavement engineering and exploring the prospects of the application (Yao, Wang et al. 2022).

There are three main types of pavement materials that can be used for lignin in pavement engineering, which are asphalt, asphalt mixture, and roadbed soil. In asphalt, lignin can be used as a modifier, extender, emulsifier, antioxidant, and coupling agent. In asphalt mixtures, lignin can be used as an additive. In road base soils, lignin can be used as a soil stabilizer(Yao, Wang et al. 2022). Furthermore, the article analyzed the application effects of lignin from the life cycle assessment. The conclusions suggest that lignin-modified asphalt exhibits more viscosity and hardness, and its high-temperature resistance and rutting resistance can be significantly improved compared with conventional asphalt. In addition, some lignin-modified asphalt binders exhibit reduced low-temperature crack resistance and fatigue resistance, which can be adjusted and selected according to the climate change in different regions. The performance of lignin as an asphalt mixture additive and asphalt extender has been proved to be feasible. Lignin can also produce good mechanical properties as well as environmental benefits as a soil stabilizer(Yao, Wang et al. 2022).

A number of papers describe the production of binderless panels manufactured with steamed fibers of various origin. The thermo-mechanical pre-treatments of the fibres have large effect on the properties of the panels. A number of chemical changes are known to occur. Autohydrolysis of the constituent cell wall polymers in the lignocellulosic fibres by the steam explosion has been

described. Especially hemicellulose polysaccharides (pentosans) degrade under these elevated temperature conditions to form furfural. The suitability of coconut fibre and pith for board production have been studied separately utilizing phenol-formaldehyde and urea-formaldehyde resins(Van Dam, van den Oever et al. 2004).

The use of lignin in wood adhesive formulations has been investigated in the past and described in numerous patents and papers, however, so far with limited commercial impact. Generally, the reactivity of the lignin released from lignocellulose after chemical and/or thermo-mechanical extraction processes is insufficient for complete substitution of synthetic resin(Karthäuser, Biziks et al. 2021). Steam explosion and organosolvlignins for that purpose would be more reactive, as compared to kraft lignin or lignosulfonates. To prepare adhesive resins from these lignins, generally, methyolation, or preferentially phenolation is required. It has been demonstrated that up to a maximum of 50% replacement of phenolic resin (PF) by (soda) lignins is possible without affecting board properties (Van Dam, van den Oever et al. 2004).

2.5 LIGNIN FROM COCONUT

Lignin isolation of Coconut coir with alkaline delignification process is to appear the highest yield of lignin which used NaOH solution concentration variety of 15%, 20%, 25%, 30%, 35 % (v/w) and time of term process started from 60 minutes, 90 minutes, 120 minutes and 150 minutes(Ding 2014). According to product presentation, yield lignin got from the comparison between the initial weight and final weight. The lowest of yield lignin is 3.72% with time term is 150 minutes and NaOH solution is 35%. The effect time process of alkaline delignification to yield lignin could be seen at. In addition to the highest yield lignin is 37.6% with timeterm is 120 minutes and it used to NaOH solution of 25%. Accordingly increasing of yield lignin concentration occurred from 60-120 minutes, in 150 minutes that yield will be diminished(Irawan, Muslimah et al. 2018).Coir based building and Packaging materials, CFC/FAO-IGHF/11) is the development of an efficient process for production of board materials from the whole coconut husk without addition of chemical binders or additives. A technology is being designed to transform the wasted residues into building boards, utilising the available high lignin content in both pith and coir fibre. The extracted coir pith was studied for binderless board production by hot pressing (Mari, 1996) and verified the effects of chemical treatments and processing conditions. It was concluded that acid treatment would be required to meet the minimum technical specifications for panels(Van Dam, van den Oever et al. 2004).

Coconut husk the fibrous external portion of the fruit of coconut palms, is a by-product of the copra extraction process and is generally considered as a waste. A variety of uses have been proposed for coconut husk lignin, which is present at levels of up to 33% by weight of the husk." The applications range from the fabrication of particle board agglomerated by "its own resin" l2 to the hydrogen chloride extraction of lignin to be used as an additive in the formulation of reinforced plastics." One important aspect that, in our view, has been omitted in these efforts is the knowledge of the approximate structure and characteristics of the lignin involved(Váquez‐Torres, Canché‐Escamilla et al. 1992).

Lignin could be isolated from a wide range of lignocellulosic waste including coconut husk. Coconut palms (Cocos nucifera L.) are abundantly grown in coastal areas of all tropical countries. The coconut processing produces a great amount of coconut husk that consists of cellulose (32.69–36.3%), hemicellulose (~22.56%) and lignin (31.9–53%) .  The lignin isolated from coconut husk can be

used as intrinsic resin. In addition, lignin has shown good potential for the manufacture of binderless thermal insulation boards , as a bio-based carbon fiber precursor, use in tablet manufacturing (pharmaceutical industry), in composite formulations, and polymer materials (such as adhesives, thermoset resins, hydrogels).  The coconut husk lignin is proposed to replace phenol partially in order to develop wood adhesives like previous works. Our past research reported on the wood adhesives developed from kenaf core (Hibiscus cannabinus) lignin and oil palm (Elaeisguineensis) fronds lignin-derived aldehyde. On top of that, the substitution of formaldehyde also becomes a major concern for the phenolic resin industry, since the formaldehyde is classified as toxic and oncogenic(Aziz, Latip et al. 2019).

Coconut coir pith is a light brown coloured, spongy, lignocellulosic waste biomaterial that is generated in huge volumes during the processing of coir fibre from coconut husks. Coir pith falls from the thick mesocarp of the coconut fruit when it is shredded during coir fibre processing, and it has a porous structure that typically consists of particles ranging from 0.2 to 2.0 mm (75% to 90%) in size. Generally, one unit-mass of coir fibre generates two unit-masses of coconut coir pith, which remains in huge quantities as a waste product with low industrial value. Characteristics of coir pith are its hydrophilic nature, absence of pathogens and renewability with no ecological drawbacks to its use due to its slow natural decomposition rate. Coir pith consists primarily of lignin cellulose, hemicelluloses and extractives, such as pectins and tannins, and the wt% content of lignin is high. These constituents primarily contain carboxyl, hydroxyl and ether groups, which makes coir pith a useful adsorbent or a natural ion exchanger. Generally, coir pith can be incinerated or dumped without any limitation. Coir pith is also used in the preparation of soilless growing media for the cultivation of some ornamental plants

and crops. Alternative, widespread usage of this lignocellulosic waste biomaterial has succeeded due to its high-water absorption and retention characteristics(Gundupalli, Kajiura et al. 2020).

2.6 EXTRACTION OF LIGNIN FROM COCONUT HUSK OR COIR

Lignin was extracted from coconut husk via Kraft and soda pulping. Kraft lignin (KL) and soda lignin (SL) were characterized to understand the HGS content, phenolic-aliphatic-OH content, molecular structure and thermal behaviour via different complementary analysis. The physico-chemical and physico-mechanical properties of LPG wood adhesives with varied loading of KL and SL were compared before further studying the influence of LDH as the nanofiller in LPG wood adhesives

CHAPTER III

MATERIALS AND METHODOLOGY

3.1 MATERIALS

Coconut husk were collected from marthandam local shop. Coconut husk were cleaned, and the waste material (husk) were dried in the open air for 7 days in the sunlight. The dried peel was milled to powder by using a mechanical grinder.

3.2 EXTRACTION OF LIGNIN

3.2.1 Acid alkali method

10g of coconut husk was mixed with 13 ml of HCL and 300 ml of distilled water. The mixture was then magnetically stirred for 1 hour at 85℃. Following this, the solution was centrifuged to separate the supernatant and the pellet, after which 300ml of distilled water was added to the pellet. Subsequently, 12g of NaOH was added, and the resulting mixture was magnetically stirred for another hour at 80℃ and combined with H2SO4. The solution was then subjected to another round of centrifugation to remove the supernatant and separate the pellet. The pellet was placed in a Petri plate and dried in a hot air oven at 70℃ overnight. Finally, the resulting product was transferred into the centrifuge tube.

3.2.2 Microwave assisted extraction

The extraction process began with 1g of powdered sample treated with water, utilizing a solid-liquid ratio (LSR) of 30:1 ml/g, an irradiation time of 60s, and a microwave power of 810W. Following extraction, the samples were allowed to reach room temperature, then filtered using Whatman no.1 filter paper and centrifuged at 5000 rpm for 10 minutes. The resulting supernatant was collected for the analysis of total phenolic content, total flavonoid content and total flavonoid content

3.3 OPTIMIZATION USING OVAT

One variable at a time (OVAT) approach is a univariate, conventional technique used for the optimization of process variables. A holistic view of the entire process parameters can be obtained using this approach. In the present study, the effect of Microwave power (270-540W), alkali concentration (2-8g) and LSR (50-200 ml/g) were optimized sequentially. One parameter was varied and other parameters were maintained at a fixed level.

The principle of heating by microwave energy is based on the direct effect of microwaves on molecules by ionic conduction and dipole rotation. Polar molecules and ionic solutions absorb microwave energy strongly because they have a permanent dipole moment (Murugesan, Maran et al. 2024). This results in the rapid rise of the temperature and fast completion of the reaction. In the second stage, after analysing the free phenolic acids and the optimal conditions of pre-treatment, it was used to carry out further steps. The time of exposure to microwaves plays a critical role. Higher power levels shall require less time and vice versa.

3.4CHARACTERIZATION

3.4.1 FTIR

The chemical composition of peel extracts of Saccharum officinarum harvested from two different geographical areas, the different extracts were scanned in the wavelength range of 515-700 nm with a resolution of 0.5 cm-1 using Spectrum Two FTIR spectrometers PerkinElmer and characteristic peaks and their functional groups were detected. FTIR peak values were recorded. Each analysis was repeated three times for spectrum confirmation.

3.5 PREPARATION OF SUNSCREEN LOTION

Three formulations F1 to F3 were prepared as per Table 1. Accurate quantities of ingredients were weighed.

3.5.1 Phase I [oil phase] ingredients (shea butter, almond oil) were heated to melt in a 100 ml beaker using hot plate. Dry powder (i.e. zinc oxide, titanium dioxide, calamine and hydroxy propyl methyl cellulose) were added to heated mixture followed by continuous heating till complete solubilization of dry powder in oil phase succeeded by addition of emulsifier’s combination (i.e. glyceryl monostearate, stearic acid, sorbitan stearate, sorbitan monooleate, PEG-20 sorbitan monolaurate and tween 80) with required HLB.

3.5.2 Phase II [aqueous phase] (rose water) was heated in separate 100 ml beaker to the same temperature as that of oil phase. Phase II was slowly poured into

Phase 1, a little at a time with constant stirring succeeded by addition of fragrance (i.e. mangosteen and mandarin berry) and color (i.e. carmoisine and erythrosine) in quantity sufficient amount. Stirring was continued in a glass mortar until a smooth and uniform paste was obtained. Rose water was added to make up the required volume.

Table 1: Composition of various sunscreen formulations.

| Ingredients (%w/v or %v/r) | F1 | F2 | F3 |
| --- | --- | --- | --- |
| Shea Butter | 5 | 10 | 10 |
| Almond oil | 15 | 30 | 30 |
| Lignin | 2.50 | 5 | 5 |
| Tween 80 | 2.50 | 5 | 5 |
| Rose water | 50 | 50 | 50 |

3.6 IN VITRO SPF ASSAY OF CREAM

SPF was determined by in-vitro method using double beam UV spectrophotometer (Systronics AU2701, India). SPF was calculated using the Eq. 1 and Normalized product function (Table 2) derived by (Arora, Sharma et al. 2015).

SPFspectrophotometric=CF290320EE(λ)×I(λ)×A(λ)     …… (1)

Where, correction factor, CF=10, EE (λ) = erythemogenic effect of radiation of wavelength, I (λ) = intensity of solar light of wavelength

A(λ) = spectrophotometric absorbance values at wavelength. All measurements were taken in triplicate and represented as mean ± SD.

Table 2: Normalized product function used in calculation of SPF

| Wavelength (nm) | EE (erythemal factor) * I (Solar Intensity) |
| --- | --- |
| 290 | 0.0150 |
| 295 | 0.0817 |
| 300 | 0.2874 |
| 305 | 0.3278 |
| 310 | 0.1864 |
| 315 | 0.0839 |
| 320 | 0.0180 |
| Total | 1 |

3.7 EVALUATION OF CREAM

3.7.1 pH of the Cream

The pH meter was calibrated using standard buffer solution. About 0.5g of the cream was weighed and dissolved in 50.0 ml of distilled water and its pH was measured.

3.7.2 Dye test

The scarlet red dye is mixed with the cream. Place a drop of the cream on a microscopic slide covers it with a cover slip, and examines it under a microscope. If the disperse globules appear red the ground colourless. The cream is o/w type. The reverse condition occurs in w/o type cream i.e. the disperse globules appear colourless in the red ground.

3.7.3 Homogeneity

The formulations were tested for the homogeneity by visual appearance and by touch.

3.7.4 Appearance

The appearance of the cream was judged by its color, pearlscence and roughness and graded.

3.7.5 After feel

Emolliency, slipperiness and amount of residue left after the application of fixed amount of cream was checked.

3.7.6 Type of smear

After application of cream, the type of film or smear formed on the skin were checked.

3.7.7 Removal

The ease of removal of the cream applied was examined by washing the applied part with tap water.

3.9.8 Irritancy test

Mark an area (1sq.cm) on the left hand dorsal surface. The cream was applied to the specified area and time was noted. Irritancy, erythema, edema, was checked if any for regular intervals up to 24 hrs and reported

3.7.9 Acid value

Take 10 gm of substance dissolved in accurately weighed, in 50 ml mixture of equal volume of alcohol and solvent ether, the flask was connected to reflux condenser and slowly heated, until sample was dissolved completely, to this 1 ml of phenolphthalein added and titrated with 0.1N NaOH, until faintly pink color appears after shaking for 30 seconds.

Acid value = n X 5.61/w

n = the number of ml of NaOH required.

w = the weigh of substance.

3.7.10 Saponification value

Introduce about 2 gm of substance refluxed with 25 ml of 0.5 N alcoholic KOH for 30 minutes, to this 1 ml of phenolphthalein added and titrated immediately, with 0.5 N HCL.

Saponification value = (b-a) X 28.05/w

The volume in ml of titrant = a

The volume in ml of titrant =b

The weigh of substance in gm = w

CHAPTER IV

RESULTS AND DISCUSSION

4.1 Lignin yield, recovery and purity

The performance of the methods for extracting lignin from coconut husk was evaluated in terms of their yield and recovery.

Table4.1:Yields and recoveries achieved in the procedures.

| Method | Yield (%) |
| --- | --- |
| Conventional | 44.45% |
| Physiochemical Method | 59.68% |

For Method I, its yield and recovery in both methods were higher than those reported by Malinsky et al (2003); Myers and Fox (1994) and Uriyapongson and Rayas Duarte (1994). These results might be due to both the fact that the husk was ground before the alkaline treatment which favored protein release in a shorter soaking stage than those taken up by Radosavljevic et al (1998)

The lignin content of the coconut husk, in the extractions was: 11.430g/100 g ± 1.3 and ….. g/100 g ± 1.1 respectively.

The highest yield and recovery was obtained by treatment microwave assisted extraction (26.80 and 59.86%) respectively. There was no correlation between total lignin and lignin yield. This was because lignin extraction was not 100 per cent efficient in any case.Extraction was said to depend on softness of the roots on harvests .According to Rahman et al, (2003), higher lignin content does not necessarily mean higher percent of extractable lignin. So, extractability of the lignin is a more important criterion in the choice of variety for starch extraction rather than starch content and he found that the average lignin recovery was found to be 80.2 per cent and 65.8 per cent in dry and wet seasons respectively.

4.2 Effect of process Variables in Extraction of Lignin (OVAT)

4.2.1 Effect of microwave power:

The effect of microwave power on lignin is significant, influencing its modification, extraction, and degradation processes. High-power microwave irradiation can induce chemical reactions in lignin, altering its molecular structure and properties. This has implications for biomass processing, pulp and paper industries, and lignocellulosic biomass utilization, where microwave-assisted methods offer potential benefits in terms of efficiency and selectivity.

Fig 4.2.1 Effect on Microwave power

4.2.2 Effect of alkali concentration:

The concentration of alkali has a significant impact on lignin-related processes, particularly in lignocellulosic biomass processing. In delignification processes, higher alkali concentrations generally result in more efficient lignin removal due to enhanced disruption of lignin-carbohydrate linkages and increased lignin solubilization. However, excessively high alkali concentrations can also lead to the degradation of lignin and cellulose, reducing the overall process efficiency and selectivity. Therefore, optimizing alkali concentration is crucial for achieving desired outcomes in lignin-related processes, balancing the need for efficient lignin removal with the preservation of cellulose integrity and product quality.

Fig 4.2.2: Effect of Alkali

4.2.3 Effect of liquid and solid ratio:

Fig 4.2.3 Effect of liquid and solid ratio:

4.3 FT-IR Lignin:

Fourier Transform Infrared Spectroscopy (FTIR) is a powerful analytical technique widely employed in the study of lignin due to its ability to provide detailed information about the chemical composition and structure of lignocellulosic materials. When applied to lignin analysis, FTIR spectroscopy reveals characteristic peaks in the spectra, each corresponding to specific functional groups and molecular vibrations within the lignin molecule. These peaks include those associated with aromatic ring stretching, aliphatic C-H stretching, carbonyl stretching, alcohol/OH stretching, and C-O stretching, among others. By analyzing the intensity, position, and shape of these peaks, researchers can gain insights into the lignin structure, composition, and potential modifications. FTIR spectroscopy thus serves as a valuable tool in various research fields, including biomass processing, pulping, and lignin valorization, providing essential information for understanding lignin's role and potential applications in sustainable biorefinery processes.

Fig 4.3.1 FTIR Lignin

4.4 Invitro SPF assay of cream

The absorbance values of formulations F1 to F10 and two marketed sunscreens (Lakme Sunexpert SPF 30 and Lakme Sunexpert SPF 24+) MS 1 and MS 2 were measured using UV spectrophotometer and SPF was calculated (Table 4 and Table 5). The results showed that F6 has highest SPF of 46.06±0.06 which may be attributed to the presence of higher concentration of zinc oxide but had residual slight whiteness left after application over skin, which could be adjusted with further formulation studies for optimization of ZnO amount F10 has an SPF value of 15.71±0.07 (medium protection sunscreen) which is sufficient for protection against sun burn for a period of about 3 h and shows better formulation characteristics. SPF determination of marketed sunscreens by in-vitro method and comparison with its claimed SPF indicated that the method is highly suitable and reliable.

4.5 Selection of optimized formulation

Formulation F1 was having less viscosity and it was interpreted that it needs addition of rheological modifier. F2 produced residual whiteness for more than 15 minutes and needs substantial reduction of concentration of zinc oxide. F3 was unstable indicated by foaming which may be due to addition of cetyl alcohol. F4 was sticky formulation and needs increased amount of emulsifier’s addition. The pH of formulation F5 was basic (pH 8) which may be due to addition of triethanolamine (TEA).

F6 was satisfactory in most aspects except optimization of ZnO and dark pink color. F7, F8, F9 and F10 were considered good formulation but due to higher viscosity and good pourability F10 was selected as optimized formulation than them.

4.6 Physicochemical studies:

The results of physicochemical properties such as color, pH, spreadability and viscosity are summarized in Table 3. The pH of formulations ranges from 6.10 (F6) to 8.34 (F5). The lotion with pH around 6.5 was considered good because it complies with skin pH. The color of formulations was acceptable pink. The viscosity of formulations ranges from 1500 (F1) to 3586 (F10)

Table 4.2 Physicochemical studies:

| Formula | Sunscreen Colour | pH (±) | Viscosity (cps) (±) | Spread ability (g.cm/sec) (±) |
| --- | --- | --- | --- | --- |
| F1 | Dark pink | 6.66 | 1500 ± 12 | 10.56 ± 0.8 |
| F2 | Pink | 6.63 | 3467 ± 13 | 29.75 ± 0.9 |
| F3 | Pink | 6.66 | 3475 ± 15 | 29.65 ± 0.7 |
| F4 | Dark Pink | 6.47 | 1787 ± 16 | 12.76 ± 0.9 |
| F5 | Dark pink | 8.34 | 3397 ± 17 | 28.65 ± 0.8 |
| F6 | Dark pink | 6.10 | 2436 ± 15 | 19.47 ± 0.7 |
| F7 | Pink | 6.49 | 2654 ± 18 | 21.57 ± 0.6 |
| F8 | Pink | 6.61 | 2166 ± 16 | 16.75 ± 0.8 |
| F9 | Pink | 6.56 | 2677 ± 15 | 21.67 ± 0.9 |
| F10 | Pink | 6.53 | 3586 ± 14 | 30.65 ± 0.7 |

The spread ability of formulations ranges from 10.56 (F1) to 30.65 (F10). The important physicochemical parameters of formulation F6 and F10 were found to be in controlled range justifying its compatibility with skin and confirming good cosmetologically property.

4.7 Stability:

Table 4.3 SPF of the formulated and marketed sunscreen:

| Formulation | SPF (±) |
| --- | --- |
| F1 | 14.73 ± 0.07 |
| F2 | 18.72 ± 0.06 |
| F3 | 16.38 ± 0.15 |
| F4 | 18.39 ± 0.07 |
| F5 | 22.65 ± 0.11 |
| F6 | 46.06 ± 0.06 |
| F7 | 18.64 ± 0.12 |
| F8 | 25.47 ± 0.07 |
| F9 | 16.15 ± 0.07 |
| F10 | 15.71 ± 0.04 |
| MS1 | 30.02 ± 0.07 |
| MS2 | 23.17 ± 0.07 |

Table4.4: Stability evaluation by physicochemical parameters (F6)

| Day | Colour | pH (±) | Viscosity (cps) (±) | Spread ability (g.cm/sec) (±) | Centrifugation at 8000 rpm |
| --- | --- | --- | --- | --- | --- |
| 0 | Dark Pink | 6.10 | 2436 ± 15 | 19.47 ± 0.7 | Stable |
| 15days (25o C& 60 %RH | Dark Pink | 6.60 | 2103 ± 12 | 17.67 ± 0.8 | Stable |
| 15days (30o C& 60 %RH | Dark Pink | 6.61 | 2095 ± 12 | 16.68 ± 0.8 | Stable |

CONCLUSION

The herbal sunscreens prepared utilizing coconut husk extracts demonstrate promising attributes indicative of their potential as effective skincare solutions. These formulations exhibit a smooth, non-granular consistency with optimal viscosity and uniform spreadability, facilitating effortless application onto the skin. Their translucent appearance, along with an agreeable pink hue and aroma, enhances their aesthetic appeal. Furthermore, these sunscreens offer commendable moisturizing properties, effectively hydrating the skin without leaving noticeable residual whiteness. They exhibit compatibility with various packaging materials and maintain stable rheology during handling, ensuring user convenience. With a skin-friendly pH level of 6.5 and no observed phase separation after centrifugation, these formulations promise gentle application and long-term stability. Beyond their sun protection factor (SPF) of 15.73, these coconut husk-based formulations are positioned to deliver additional skincare benefits, including emollience, anti-aging, and anti-wrinkle effects, underscoring their potential as multifaceted and efficacious skincare products.

REFERENCE

- Antunes, F., I. F. Mota, J. da Silva Burgal, M. Pintado and P. S. Costa (2022). "A review on the valorization of lignin from sugarcane by-products: From extraction to application." Biomass and Bioenergy 161: 106603.

- Ariyanta, H. A., E. B. Santoso, L. Suryanegara, E. T. Arung, I. W. Kusuma, M. N. A. M. Taib, M. H. Hussin, Y. Yanuar, I. Batubara and W. Fatriasari (2023). "Recent progress on the development of lignin as future ingredient biobased cosmetics." Sustainable Chemistry and Pharmacy  32: 100966.

- Arora, S., N. Sharma, A. Mahajan, J. Kaur and S. Singh (2015). "Development, physicochemical characterization and in-vitro evaluation of herbal sunscreen lotion." Journal of Pharmaceutical Technology, Research and Management 3(2): 113-125.

- Aziz, N. A., A. F. A. Latip, L. C. Peng, N. H. Abd Latif, N. Brosse, R. Hashim and M. H. Hussin (2019). "Reinforced lignin-phenol-glyoxal (LPG) wood adhesives from coconut husk." International journal of biological macromolecules  141: 185-196.

- Chio, C., M. Sain and W. Qin (2019). "Lignin utilization: A review of lignin depolymerization from various aspects." Renewable and sustainable energy reviews  107: 232-249.

- de la Torre, M. J., A. Moral, M. D. Hernández, E. Cabeza and A. Tijero (2013). "Organosolv lignin for biofuel." Industrial crops and products 45: 58-63.

- Ding, T. Y. (2014). Production of bioethanol by using pretreated coconut husk as carbon source, UTAR.

- Domínguez-Rodríguez, G., M. L. Marina and M. Plaza (2017). "Strategies for the extraction and analysis of non-extractable polyphenols from plants." Journal of Chromatography A 1514: 1-15.

- Emerit, I. (1992). "Free radicals and aging of the skin." Free radicals and aging: 328-341.

- Erdocia, X., F. Hernández-Ramos, A. Morales, N. Izaguirre, P. L. de Hoyos-Martínez and J. Labidi (2021). Lignin extraction and isolation methods. Lignin-Based Materials for Biomedical Applications, Elsevier: 61-104.

- Espinoza-Acosta, J. L. and E. G. Figueroa-Espinoza (2022). "Recent Progress in the Production of Lignin-based Sunscreens: A Review." BioResources 17(2).

- Fernandez de Simon, B., E. Esteruelas, Á. M. Muñoz, E. Cadahía and M. Sanz (2009). "Volatile compounds in acacia, chestnut, cherry, ash, and oak woods, with a view to their use in cooperage." Journal of Agricultural and Food Chemistry 57(8): 3217-3227.

- Ganguly, B., M. Hota and J. Pradhan (2021). "Skin aging: Implications of UV radiation, reactive oxygen species and natural antioxidants." Reactive Oxygen Species: 1-21.

- Gasparro, F. P. (2000). "Sunscreens, skin photobiology, and skin cancer: the need for UVA protection and evaluation of efficacy." Environmental Health Perspectives 108(suppl 1): 71-78.

- Gavrilescu, D. (2020). "Pulping fundamentals and processing." Pulp Production and Processing: High-Tech Applications: 19.

- Gellerstedt, G. (2015). "Softwood kraft lignin: Raw material for the future." Industrial Crops and Products 77: 845-854.

- Gomes da Silva, F. J., R. M. Gouveia, F. J. Gomes da Silva and R. M. Gouveia (2020). "Sustainable production cases." Cleaner Production: Toward a Better Future: 281-373.

- Gundupalli, M. P., H. Kajiura, T. Ishimizu and D. Bhattacharyya (2020). "Alkaline hydrolysis of coconut pith: process optimization, enzymatic saccharification, and nitrobenzene oxidation of Kraft lignin." Biomass Conversion and Biorefinery: 1-19.

- Henriksson, N. and K. Nordell (2023). "Lignin in Cosmetics: State of the Art: Discerning the value of lignin in the cosmetic industry."

- Irawan, D., N. Muslimah and Z. Arifin (2018). "Lignin isolation from coconut coir with variation of time and concentration of NaOH in the process of alkaline delignification." Chemical 11(4): 1458-1460.

- Jardim, J. M., P. W. Hart, L. Lucia and H. Jameel (2020). "Insights into the potential of hardwood kraft lignin to be a green platform material for emergence of the biorefinery." Polymers 12(8): 1795.

- Karić, N., A. S. Maia, A. Teodorović, N. Atanasova, G. Langergraber, G. Crini, A. R. Ribeiro and M. Đolić (2022). "Bio-waste valorisation: Agricultural wastes as biosorbents for removal of (in) organic pollutants in wastewater treatment." Chemical Engineering Journal Advances 9: 100239.

- Karthäuser, J., V. Biziks, C. Mai and H. Militz (2021). "Lignin and lignin-derived compounds for wood applications—A review." Molecules 26(9): 2533.

- Kim, T. H., S. H. Park, S. Lee, A. S. Bharadwaj, Y. S. Lee, C. G. Yoo and T. H. Kim (2023). "A review of biomass-derived UV-shielding materials for bio-composites." Energies 16(5): 2231.

- Konduri, M. K. and P. Fatehi (2015). "Production of water-soluble hardwood kraft lignin via sulfomethylation using formaldehyde and sodium sulfite." ACS Sustainable Chemistry & Engineering 3(6): 1172-1182.

- Margarida Martins, M., F. Carvalheiro and F. Gírio (2024). "An overview of lignin pathways of valorization: From isolation to refining and conversion into value-added products." Biomass Conversion and Biorefinery 14(3): 3183-3207.

- Mat, K., Z. Abdul Kari, N. D. Rusli, H. Che Harun, L. S. Wei, M. M. Rahman, H. N. Mohd Khalid, M. H. Mohd Ali Hanafiah, S. A. Mohamad Sukri and R. I. A. Raja Khalif (2022). "Coconut palm: food, feed, and nutraceutical properties." Animals 12(16): 2107.

- Ngoc, L. T. N., V. V. Tran, J.-Y. Moon, M. Chae, D. Park and Y.-C. Lee (2019). "Recent trends of sunscreen cosmetic: An update review." Cosmetics 6(4): 64.

- Novaes, E., M. Kirst, V. Chiang, H. Winter-Sederoff and R. Sederoff (2010). "Lignin and biomass: a negative correlation for wood formation and lignin content in trees." Plant physiology 154(2): 555-561.

- Oliveira, M. B., I. B. Valentim, T. R. Santos, J. A. Xavier, J. N. Ferro, E. O. Barreto, A. E. Santana, L. V. Melo, C. B. Bottoli and M. O. Goulart (2021). "Photoprotective and antiglycation activities of non-toxic Cocos nucifera Linn.(Arecaceae) husk fiber ethanol extract and its phenol chemical composition." Industrial Crops and Products 162: 113246.

- Peracchi, L. M., R. Panahabadi, J. Barros-Rios, L. E. Bartley and K. A. Sanguinet (2024). "Grass lignin: biosynthesis, biological roles, and industrial applications." Frontiers in Plant Science 15: 1343097.

- Piccinino, D. (2019). "Green chemistry and bio-nanotechnology: design of polyphenols in biocatalysis, functionalized nanomaterials and bio-based product."

- Quesada-Medina, J., F. J. López-Cremades and P. Olivares-Carrillo (2010). "Organosolv extraction of lignin from hydrolyzed almond shells and application of the δ-value theory." Bioresource technology (21): 8252-8260.

- Salunkhe, D. and S. Kadam (1995). Coconut. Handbook of Fruit Science and Technology, CRC Press: 501-524.

- Sari, D. N., M. F. Rois, W. Widiyastuti and H. Setyawan (2022). Organosolv lignin from coconut coir as potential biomaterials for sunscreen. AIP Conference Proceedings, AIP Publishing.

- Sen Mandi, S. and S. Sen Mandi (2016). "Effect of UV radiation on life forms." Natural UV Radiation in Enhancing Survival Value and Quality of Plants: 23-43.

- Souza, R., F. Gomes, E. Brito and R. Costa Lelis (2020). "A review on lignin sources and uses." J Appl Biotechnol Bioeng 7(3): 100-105.

- Tran, M. H., D.-P. Phan and E. Y. Lee (2021). "Review on lignin modifications toward natural UV protection ingredient for lignin-based sunscreens." Green Chemistry 23(13): 4633-4646.

- Upton, B. M. and A. M. Kasko (2016). "Strategies for the conversion of lignin to high-value polymeric materials: review and perspective." Chemical reviews 116(4): 2275-2306.

- Van Dam, J. E., M. J. van den Oever, W. Teunissen, E. R. Keijsers and A. G. Peralta (2004). "Process for production of high density/high performance binderless boards from whole coconut husk: Part 1: Lignin as intrinsic thermosetting binder resin." Industrial Crops and products 19(3): 207-216.

- Vanholme, R., B. Demedts, K. Morreel, J. Ralph and W. Boerjan (2010). "Lignin biosynthesis and structure." Plant physiology 153(3): 895-905.

- Váquez‐Torres, H., G. Canché‐Escamilla and C. Cruz‐Ramos (1992). "Coconut husk lignin. I. Extraction and characterization." Journal of applied polymer science 45(4): 633-644.

- Vieira, F., H. E. Santana, M. Jesus, J. Santos, P. Pires, M. Vaz-Velho, D. P. Silva and D. S. Ruzene (2024). "Coconut Waste: Discovering Sustainable Approaches to Advance a Circular Economy." Sustainability 16(7): 3066.

- Wang, H., Y. Pu, A. Ragauskas and B. Yang (2019). "From lignin to valuable products–strategies, challenges, and prospects." Bioresource technology 271: 449-461.

- Widsten, P. (2020). "Lignin-based sunscreens—State-of-the-art, prospects and challenges." Cosmetics 7(4): 85.

- Wypych, G. (2020). Handbook of UV degradation and stabilization, Elsevier.

- Yang, Y., A. Iqba and R.Qadri (2018)."Breeding of coconut (Cocos Nucifera L.): The tree of life." Advances in Plant Breeding Strategies: Fruits: Volume 3: 673-725.

- Yao, H., Y. Wang, J. Liu, M. Xu, P. Ma, J. Ji and Z. You (2022). "Review on applications of lignin in pavement engineering: a recent survey." Frontiers in Materials 8: 803524.

- Zhang, L., A. Larsson, A. Moldin and U. Edlund (2022). "Comparison of lignin distribution, structure, and morphology in wheat straw and wood." Industrial Crops and Products 187: 115432.